## Slide 1: Acta E Articles: Frequently Encountered Problems and Hints for Evaluating Structures of Inorganic and Metal-Organic Compounds
Matthias Weil
mweil@mail.zserv.tuwien.ac.at

## Slide 2
Category
Although the wrong category is a minor problem (without
consequences; the wrong category is usually corrected at the proof
stage by technical editors or section editors), co-editors are
encouraged to check the correct category:
_publ_requested_category
EI for inorganics
(no C─C and/or C─H bonds)
EM for metal organics
(at least one metal and C─C and/or C─H bonds must be present)
EO for organics
(no metals, but semi-metals like Se, Te can be present)

## Slide 3
Disorder
An easy way to check disorder: Just look into the review *.pdf
Treatment of disorder should be reported in the Abstract with
numerical values for the occupancies (including s.u.) and in more
detail in _publ_section_exptl_refinement
Key indicators in the published paper

## Slide 4
Special positions
Special positions or symmetry should be reported in the Abstract!
How to spot special positions in an easy way?
Check coordinates in the review *.pdf  Wyckoff positions in IT A
E.g. : … the Fe(II) atom is located on an inversion centre …;
… the MgO6 octahedron has .m. symmetry …
But not: The asymmetric unit contains one ligand molecule and
half of a metal atom (there are no half-/quater/- etc. atoms!)
Or check the structure visually with PLATON
or the freely downloadable Mercury

## Slide 5
http://www.ccdc.cam.ac.uk/products/mercury/
Load CIF
Display
Symmetry Elements

## Slide 6
http://www.ccdc.cam.ac.uk/products/mercury/
Load CIF
Display
Symmetry Elements
N,N'-Dimethylethylenediammonium dioxalatocuprate(II)

## Slide 7
http://www.ccdc.cam.ac.uk/products/mercury/
Load CIF
Display
Symmetry Elements
N,N'-Dimethylethylenediammonium dioxalatocuprate(II)
Inversion symmetry cation
N,N'-Dimethylethylenediammonium dioxalatocuprate(II)

## Slide 8
http://www.ccdc.cam.ac.uk/products/mercury/
Load CIF
Display
Symmetry Elements
N,N'-Dimethylethylenediammonium dioxalatocuprate(II)
Inversion symmetry cation
N,N'-Dimethylethylenediammonium dioxalatocuprate(II)
Inversion symmetry
dimeric complex
Tetrakis(μ2-2-phenoxypropionato-κ3-O,O‚O‘‚-κ3O,O,O,-κ4O,O‚)-bis[(2-phenoxypropionato-κ2-O,O')(1,10-phenanthroline-κ2-N,N‘) gadolinium(III)]

## Slide 9
http://www.ccdc.cam.ac.uk/products/mercury/
Load CIF
Display
Symmetry Elements
N,N'-Dimethylethylenediammonium dioxalatocuprate(II)
Inversion symmetry cation
N,N'-Dimethylethylenediammonium dioxalatocuprate(II)
Inversion symmetry
dimeric complex
Tetrakis(μ2-2-phenoxypropionato-κ3-O,O‚O‘‚-κ3O,O,O,-κ4O,O‚)-bis[(2-phenoxypropionato-κ2-O,O')(1,10-phenanthroline-κ2-N,N‘) gadolinium(III)]
Mirror symmetry
for the entire complex
Bis(3-methylpyridine- κN)bis(thiocyanato- κN)zinc

## Slide 10
Report coordination number(s) and/or corresponding polyhedra for
metal atoms in the Abstract. This can be supplemented by flagged
metal—ligand atom distances to be published in Table 1
Mn OH3 1.9149(11) 3_665 y
Mn OH3 1.9149(11) 8_455 ?
Mn OH3 1.9149(11) 1_455 ?
Mn OH3 1.9149(11) 2_545 ?
Mn OH3 1.9149(11) 7_545 ?
Mn OH3 1.9149(11) 9_665 ?
Ca O2 2.3465(11) 4 y
Ca O2 2.3465(11) . ?
Ca OH3 2.456(5) 3_665 y
Ca OH3 2.456(5) 6_665 ?
Ca OH3 2.518(5) 1_455 ?
Ca OH3 2.518(5) 4_455 y
Ca OW4 2.578(9) . y
Ca OW4 2.690(9) 3_565 y
Symmetry-related distances should not be flagged since point group
symmetries of the polyhedra should be indicated in the Abstract in any
event. Angles around metal atoms are usually of no great insight.
Coordination numbers and polyhedra

## Slide 11
Coordination polyhedra (coordination numbers) are very good
measures for the correctness of a metal! Some metal ions are known
to have peculiar coordination polyhedra (and vice versa):
CN = 3
Trigonal-planar (T-shaped) coordination for ions like Ag(I), Cu(I), …
CN = 4
 Tetrahedral coordination for ions like Li(I), Co(II), Al(III), Sn(IV), …
 Square-planar coordination frequent for d8 ions (Ni(II), Pt(II), Pd(II));
sometimes for Cu(II) apparent from the *.lst file when long distances
are not recognized (‚low‘ CONN instruction in SHELXL); extremely
unusual (if existing at all) for ions like Fe(II/III), Co(II/III), Zn(II), …
CN = 2
Linear coordination for ions like Ag(I), Hg(II), Au(I) …
Coordination numbers and polyhedra

## Slide 12
CN = 5
 Trigonal-bipyramidal coordination for ions like Al(III), Sn(IV), Zn(II), …
 Square-pyramidal coordination for ions like Cu(II), Ni(II), V(V), …
CN = 6
 Octahedral coordination for ions like Mg(II), Al(III), Mn(II), Cr(III), …
Jahn-Teller effect results in a considerably tetragonally distorted
octahedron ([4+2] coordination with two long metal-ligand distances)
and is pronounced for ions Mn(III), Cr(II), Cu(II)
 Trigonal-prismatic coordination for ions like Mo(VI), Zr(IV), …
CN  7
Frequently very distorted polyhedra for ions with larger ionic radius
like Na(I), Ca(II), RE(III), …
Coordination numbers and polyhedra

## Slide 13
Other very useful criteria to check the correctness of a metal:
Bond lengths!
Inorganics: Bergerhoff & Brandenburg, Int. Tables C, p 771-780.
Metal-organics: Orpen et al., Int. Tables C, p 804-888.
Bond valence sums (BVS)!
N.E. Brese & M. O'Keeffe (1991). Acta Cryst. B47, 192-197.
I.D. Brown (2002). The chemical bond in inorganic chemistry :
the bond valence model. IUCr Monographs in Crystallography 12
Software available for calculation of BVS:
http://www.ccp14.ac.uk/solution/bond_valence/index.html
PLATON also allows to calculate BVS

## Slide 14
Crystallographic directions
In the Abstract, crystal packing features in terms of chain or layer
formation are discussed, e.g.
– „ …and the metal atoms are bridged by the oxalate ligands,
resulting in the formation of a helical chain.“
- „Intermolecular O –H…O hydrogen bonding interactions lead to a
two-dimensional set up.“
Such features should always be completed by indicating the
crystallographic directions:
„… of a helical chain extending parallel to [100] (to the a axis)“
[brackets denote a direction vector]
„ …to a two-dimensional set up parallel to (100) (to the bc plane)“
(parentheses denote planes)

## Slide 15
In the CIF the order
N1 Pd 2.072(9) . ?
N1 H1 0.85(2) . ?
N2 Pd 2.005(11) . ?
N2 H10 0.85(2) . ?
O1 Pd 1.976(8) . ?
O3 H8 0.86(2) . ?
O5 Pd 2.024(7) . ?
...
is often confusing
Order of atoms
whereas the order
Pd O1 1.976(8) . ?
Pd N2 2.005(11) . ?
Pd O5 2.024(7) . ?
Pd N1 2.0724(9) . ?
O1 C1 1.307(14) . ?
O2 C1 1.244(14) . ?
O3 C5 1.317(7) . ?
...
is much clearer
Order of atoms in SHELXL *.ins (JANA *.m50) [or re-refining with PLATON]
Metal1
Metal2
Ligand atom1
Ligand atom 2
...

## Slide 16
Crystal colour
Check consistency:
_publ_section_exptl_prep
;
… . Slow evaporation of the filtrate overnight resulted in
green cystals suitable for X-ray analysis in approximately 70% yield.
;
BUT
_exptl_crystal_colour brown
Ask authors when crystal colour seems to be ‚wrong‘ !
Provides useful information, although in some cases ambiguous!

## Slide 17
Ox. State | 57 | 58 | 59 | 60 | 61 | 62 | 63 | 64 | 65 | 66 | 67 | 68 | 69 | 70 | 71
+2 |  |  |  |  |  | Sm2+ | Eu2+ |  |  |  |  |  | Tm2+ | Yb2+ | 
+3 | La3+ | Ce3+ | Pr3+ | Nd3+ | Pm3+ | Sm3+ | Eu3+ | Gd3+ | Tb3+ | Dy3+ | Ho3+ | Er3+ | Tm3+ | Yb3+ | Lu3+
+4 |  | Ce4+ | Pr4+ | Nd4+ |  |  |  |  | Tb4+ | Dy4+ |  |  |  |  | 
Ions with closed-shell electronic configuration (row I; row II; Zn, Cd, Hg)
most frequently are colourless, except for charge-transfer complexes or where
anions are coloured, e.g. for chromates(VI)
Some first row transition metal ions are ‚chameleons‘ . They can adopt colours in the
entire spectral range, depending on the ligand , e.g. Cu(II), Ni(II).
Crystal colour
Rare earth ions are difficult to classify in terms of colour. Here are the most frequently
observed colours:
Colour may serve as a warning sign for an incorrect metal, e.g.
‚coloured‘ Zn-compounds; colourless Cu(II)-compounds, etc.

## Slide 18
Rare earth metals
Often reported in form of isotypic series
Correctness of the metal is difficult to check (refinement of s.o.f. ambiguous)
Use the Check for similar reduced cells option provided at your homepage to
search for isotypic structures and consider the lanthanide contraction:
Deviation of the expected decrease of the unit cell volume with increasing atom
number is a clear warning sign!
In such cases check the deposited structure factors for similarity with PLATON

## Slide 19
Conclusion and Recommendation
For validation, use checkCIF output provided in the review *.pdf
or at your homepage
It is recommended to always re-refine the structure ( occupancies of
metal atoms, location of H atoms from difference Fourier maps etc.)
– just a few mouse clicks / keys with PLATON!
Using programs and tools like/within PLATON, publCIF, Mercury,
etc. will make your life easier!
Nevertheless, always consider your chemical intuition!
Thanks to all of you for your work and input for the journal!